Extended Data Table 2: Plasma surface functionalisation: Conditions for the respective plasma surface functionalisation with air, TMS, and PFAC–6.

| Gas/Monomer | Power / W | Pressure / mbar | Duration / s |
| --- | --- | --- | --- |
| Air | 20 | 0.2 | 60 |
| TMS | 3 | 0.2 | 180 |
| PFAC–6 | 50 (peak) | 0.2 | Pulsed |