## Chemicals & Materials Used

Table 1: List of chemicals and materials used.

| Chemical / Material | Supplier | Batch / Catalogue Number |
| --- | --- | --- |
| Perfluorotributylamine (Fluorinert FC-43) | 3M Inc. | 040005 / ZF-0002-1306-4 |
| Methacryloyl functionalised silica nanoparticles (Aerosil R711®) | Evonik Industries | 4040235 |
| Zinc oxide nanopowder | Sigma-Aldrich Ltd. | MKBV5880V / 544906 |
| Graphene nanoplatelets | Strem Chemicals UK Ltd | 30334300 |
| Trifluoroacetic acid | Fluorochem Ltd. | 4A-93-15 |
| Propan-2-ol | Fisher Scientific Ltd. | P/7490/17 |
| Cyclohexane | Sigma-Aldrich Ltd. | 227048 |
| Ultrahigh-purity water | Analytical laboratory | B.S. 3978 grade 1 |
| Hexadecane | Sigma-Aldrich Ltd. | STBF 4225V / H6703 |
| Glass microscope slides | Academic Science Ltd. | N/A 141 |
| Silicon (100) wafers | Silicon Valley Microelectronics Inc. | H9100 0302 |