| Sample Description | Lab Book Reference | Date | Instrument Filename |
| --- | --- | --- | --- |
|  |  |  | XRD |
| Glass only | HJC-331 | 26/10/20 | d7_17601 |
| Tea-cinnamaldehyde coating on glass | HJC-331 | 26/10/20 | d7_17602 |
| Tea-cinnamaldehyde-silver coating on glass | HJC-331 | 26/10/20 | d7_17603 |
| Tea-cinnamaldehyde-copper coating on glass | HJC-331 | 26/10/20 | d7_17604 |