| Sample Description | Lab Book Reference | Date |
| --- | --- | --- |
| Poly(diallyldimethylammonium)–anionic fluorosurfactant coated silicon wafer substrate | AR220 | 31/05/17 |
| Poly(diallyldimethylammonium)–1% w/v silica (7 nm)–anionic fluorosurfactant coated silicon wafer substrate | AR221 | 31/05/17 |
| Poly(diallyldimethylammonium)–2% w/v silica (7 nm)–anionic fluorosurfactant coated silicon wafer substrate | AR222 | 31/05/17 |
| Poly(diallyldimethylammonium)–3% w/v silica (7 nm)–anionic fluorosurfactant coated silicon wafer substrate | AR223 | 31/05/17 |