# 23srv389

| Table 1 Crystal data and structure refinement for 23srv389. |  |
| --- | --- |
| Identification code | 23srv389 |
| Empirical formula | C24H34N6O2 |
| Formula weight | 438.57 |
| Temperature/K | 100.00 |
| Crystal system | tetragonal |
| Space group | P42/n |
| a/Å | 22.73260(8) |
| b/Å | 22.73260(8) |
| c/Å | 9.27575(5) |
| α/° | 90.00000000000001 |
| β/° | 90.00000000000003 |
| γ/° | 90.00000000000003 |
| Volume/Å3 | 4793.44(3) |
| Z | 8 |
| ρcalcg/cm3 | 1.215 |
| μ/mm-1 | 0.224 |
| F(000) | 1888.0 |
| Crystal size/mm3 | 0.101 × 0.006 × 0.005 |
| Radiation | Synchrotron (λ = 1.0402) |
| 2Θ range for data collection/° | 3.708 to 80.23 |
| Index ranges | -27 ≤ h ≤ 27, -27 ≤ k ≤ 27, -11 ≤ l ≤ 11 |
| Reflections collected | 36588 |
| Independent reflections | 4675 [Rint = 0.1107, Rsigma = 0.0620] |
| Data/restraints/parameters | 4675/18/364 |
| Goodness-of-fit on F2 | 0.932 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0400, wR2 = 0.0950 |
| Final R indexes [all data] | R1 = 0.0574, wR2 = 0.0985 |
| Largest diff. peak/hole / e Å-3 | 0.19/-0.14 |

| Table 2 Fractional Atomic Coordinates (×104) and Equivalent Isotropic Displacement Parameters (Å2×103) for 23srv389. Ueq is defined as 1/3 of the trace of the orthogonalised UIJ tensor. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Atom | x | y | z | U(eq) |
| O1 | 4704.2(5) | -1103.0(4) | 9069.3(11) | 37.5(3) |
| O2 | 5179.8(4) | 1659.1(4) | 5965.9(11) | 28.2(2) |
| N1 | 7230.0(7) | -826.1(9) | 9024.6(17) | 64.7(5) |
| N2 | 5325.9(6) | -1479.3(6) | 7382.9(16) | 36.4(3) |
| N3 | 4402.3(6) | -1177.9(5) | 6724.9(15) | 32.0(3) |
| N4 | 4814.7(5) | 1084.1(5) | 7776.4(15) | 30.7(3) |
| N5 | 5529.8(5) | 1759.5(6) | 8252.4(15) | 32.0(3) |
| N6 | 7157(2) | 1234(2) | 6129(6) | 43.4(13) |
| N6A | 7268(2) | 1473(2) | 5895(6) | 50.1(13) |
| C4 | 7042.8(8) | -274.7(11) | 9136(2) | 60.9(6) |
| C3 | 6460.9(7) | -104.4(9) | 9010.3(19) | 49.2(5) |
| C2 | 6042.8(7) | -536.0(7) | 8768.6(17) | 40.8(4) |
| C1 | 6216.0(7) | -1118.7(8) | 8655.2(17) | 41.2(4) |
| C5 | 6813.3(8) | -1229.8(10) | 8798.7(19) | 55.7(5) |
| C6 | 5787.2(7) | -1614.7(7) | 8408.9(19) | 44.1(4) |
| C7 | 4800.8(7) | -1243.0(6) | 7794.9(17) | 32.7(4) |
| C8 | 3866.5(6) | -834.8(6) | 6893.5(16) | 30.6(3) |
| C9 | 3909.0(6) | -199.0(6) | 6316.6(16) | 28.1(3) |
| C10 | 3300.7(6) | 87.2(6) | 6549.5(16) | 29.8(3) |
| C11 | 3253.6(6) | 760.4(6) | 6389.0(16) | 27.9(3) |
| C12 | 3753.4(6) | 1050.7(6) | 7252.9(16) | 28.6(3) |
| C13 | 4359.5(6) | 798.6(6) | 6915.9(16) | 27.3(3) |
| C14 | 4372.7(6) | 138.6(6) | 7192.9(16) | 28.3(3) |
| C15 | 4081.2(6) | -222.1(6) | 4714.5(17) | 34.0(4) |
| C16 | 3271.7(6) | 965.5(6) | 4814.6(17) | 32.0(3) |
| C17 | 2659.5(6) | 951.3(7) | 7015.4(17) | 33.7(4) |
| C18 | 5174.6(6) | 1508.4(6) | 7252.6(16) | 26.2(3) |
| C19 | 5993.7(6) | 2167.5(7) | 7865.2(18) | 35.7(4) |
| C20 | 6607(3) | 1965(2) | 7467(6) | 24.1(14) |
| C20A | 6546(3) | 1782(2) | 7633(7) | 25.0(11) |
| C21 | 7116.4(12) | 2172.9(12) | 8060(3) | 33.6(8) |
| C21A | 6864.9(12) | 1516.3(12) | 8719(3) | 34.1(8) |
| C22 | 7648.7(13) | 1912.7(13) | 7690(3) | 33.8(8) |
| C22A | 7385.5(13) | 1228.9(13) | 8385(4) | 39.7(8) |
| C23 | 7644(3) | 1452(2) | 6736(6) | 36.6(13) |
| C23A | 7563(3) | 1218(2) | 6971(7) | 46.3(14) |
| C24 | 6653(2) | 1502.0(19) | 6522(5) | 37.0(12) |
| C24A | 6769(2) | 1750(2) | 6266(5) | 39.3(11) |

| Table 3 Anisotropic Displacement Parameters (Å2×103) for 23srv389. The Anisotropic displacement factor exponent takes the form: -2π2[h2a*2U11+2hka*b*U12+…]. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Atom | U11 | U22 | U33 | U23 | U13 | U12 |
| O1 | 49.6(6) | 42.5(6) | 20.4(6) | 1.3(5) | 2.6(5) | 11.2(5) |
| O2 | 31.6(5) | 32.7(5) | 20.3(6) | -0.5(4) | -0.1(4) | 0.4(4) |
| N1 | 43.9(10) | 118.7(16) | 31.7(9) | 1.7(10) | -0.9(7) | 12.8(10) |
| N2 | 46.6(8) | 39.6(8) | 22.9(8) | -1.5(6) | 3.4(6) | 12.6(6) |
| N3 | 41.6(7) | 33.5(7) | 21.1(7) | -0.2(6) | 2.8(6) | 7.0(5) |
| N4 | 31.3(7) | 40.7(7) | 20.2(7) | 4.3(6) | -1.8(5) | -0.8(5) |
| N5 | 36.1(7) | 36.6(7) | 23.4(7) | -2.1(6) | -3.2(6) | 1.7(5) |
| N6 | 32(2) | 61(4) | 38(3) | -16(2) | -2.3(18) | 5(2) |
| N6A | 42(3) | 69(4) | 39(2) | -9(2) | 4(2) | 19(2) |
| C4 | 43.4(11) | 112.1(18) | 27.2(11) | -0.6(11) | -1.0(8) | -9.6(11) |
| C3 | 47.1(11) | 74.5(12) | 25.8(9) | 0.6(9) | 1.2(8) | -5.2(9) |
| C2 | 37.4(9) | 64.2(11) | 20.8(8) | 3.8(8) | 1.7(7) | 3.7(8) |
| C1 | 41.8(9) | 62.9(11) | 18.9(8) | 5.1(7) | 2.6(7) | 16.6(8) |
| C5 | 49.1(11) | 95.4(15) | 22.6(10) | 5.2(9) | 2.1(8) | 23.3(11) |
| C6 | 53.0(10) | 49.0(10) | 30.4(9) | 5.3(8) | 3.2(8) | 21.8(8) |
| C7 | 45.3(9) | 28.5(8) | 24.2(9) | 4.4(6) | 4.2(7) | 5.0(7) |
| C8 | 35.5(8) | 33.4(8) | 22.8(8) | 0.4(6) | 4.8(6) | 2.0(6) |
| C9 | 32.1(8) | 31.4(8) | 20.8(8) | 2.3(6) | 3.0(6) | 3.1(6) |
| C10 | 30.1(8) | 35.9(8) | 23.4(8) | 1.1(6) | 2.4(6) | -1.5(6) |
| C11 | 27.9(8) | 34.6(8) | 21.1(8) | 1.5(6) | 0.5(6) | 3.4(6) |
| C12 | 32.6(8) | 31.5(8) | 21.7(8) | 0.5(6) | -0.6(6) | 3.3(6) |
| C13 | 28.9(8) | 34.1(8) | 19.0(8) | 2.5(6) | -0.2(6) | -0.6(6) |
| C14 | 28.3(7) | 33.1(8) | 23.5(8) | 4.7(6) | 4.7(6) | 3.5(6) |
| C15 | 39.5(8) | 37.2(8) | 25.4(9) | 3.1(7) | 4.7(7) | 6.3(7) |
| C16 | 33.2(8) | 36.5(8) | 26.2(9) | 2.3(7) | -1.7(6) | 3.5(6) |
| C17 | 31.8(8) | 41.5(9) | 27.9(9) | 0.8(7) | 0.3(6) | 4.1(6) |
| C18 | 25.1(7) | 30.0(8) | 23.4(8) | -1.6(6) | -0.2(6) | 8.8(6) |
| C19 | 28.9(8) | 44.8(9) | 33.3(9) | -11.9(7) | -1.5(7) | 2.9(7) |
| C20 | 29(2) | 19(3) | 24(2) | 3.6(19) | 0.0(17) | -4(2) |
| C20A | 25(2) | 22(3) | 28(2) | -3(2) | 0.9(16) | -7(2) |
| C21 | 33.5(18) | 29.9(17) | 38(2) | -1.9(14) | -4.1(14) | -6.7(13) |
| C21A | 34.0(16) | 37.7(17) | 30.6(18) | 2.5(13) | 2.7(13) | 4.4(12) |
| C22 | 27.4(17) | 36.7(18) | 37(2) | 1.3(15) | -3.8(14) | -4.0(13) |
| C22A | 38.1(17) | 42.6(18) | 38(2) | 6.1(15) | -4.2(15) | 8.7(14) |
| C23 | 26(2) | 52(4) | 32(3) | 0(2) | 0.3(18) | 10(2) |
| C23A | 38(3) | 54(4) | 47(3) | -3(3) | -2(2) | 17(3) |
| C24 | 26(2) | 48(3) | 38(3) | -16(2) | -5.6(18) | 1(2) |
| C24A | 37(3) | 50(3) | 31(2) | 1(2) | -4.2(17) | 7(2) |

| Table 4 Bond Lengths for 23srv389. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Atom | Atom | Length/Å |  | Atom | Atom | Length/Å |
| O1 | C7 | 1.2437(17) |  | C8 | C9 | 1.5442(19) |
| O2 | C18 | 1.2418(17) |  | C9 | C10 | 1.5434(19) |
| N1 | C4 | 1.328(3) |  | C9 | C14 | 1.536(2) |
| N1 | C5 | 1.335(3) |  | C9 | C15 | 1.538(2) |
| N2 | C6 | 1.449(2) |  | C10 | C11 | 1.5414(19) |
| N2 | C7 | 1.3637(19) |  | C11 | C12 | 1.5389(19) |
| N3 | C7 | 1.352(2) |  | C11 | C16 | 1.534(2) |
| N3 | C8 | 1.4550(18) |  | C11 | C17 | 1.5330(19) |
| N4 | C13 | 1.4591(18) |  | C12 | C13 | 1.5248(19) |
| N4 | C18 | 1.3548(18) |  | C13 | C14 | 1.5226(19) |
| N5 | C18 | 1.3557(19) |  | C19 | C20 | 1.514(7) |
| N5 | C19 | 1.450(2) |  | C19 | C20A | 1.545(6) |
| N6 | C23 | 1.338(8) |  | C20 | C21 | 1.366(7) |
| N6 | C24 | 1.346(7) |  | C20 | C24 | 1.375(8) |
| N6A | C23A | 1.335(8) |  | C20A | C21A | 1.381(6) |
| N6A | C24A | 1.343(7) |  | C20A | C24A | 1.368(7) |
| C4 | C3 | 1.383(2) |  | C21 | C22 | 1.390(4) |
| C3 | C2 | 1.384(2) |  | C21A | C22A | 1.387(4) |
| C2 | C1 | 1.386(2) |  | C22 | C23 | 1.372(7) |
| C1 | C5 | 1.388(2) |  | C22A | C23A | 1.373(7) |
| C1 | C6 | 1.508(2) |  |  |  |  |

| Table 5 Bond Angles for 23srv389. |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Atom | Atom | Atom | Angle/˚ |  | Atom | Atom | Atom | Angle/˚ |
| C4 | N1 | C5 | 115.70(17) |  | C16 | C11 | C12 | 110.22(11) |
| C7 | N2 | C6 | 122.22(14) |  | C17 | C11 | C10 | 107.80(11) |
| C7 | N3 | C8 | 122.73(13) |  | C17 | C11 | C12 | 109.37(12) |
| C18 | N4 | C13 | 123.27(13) |  | C17 | C11 | C16 | 107.37(11) |
| C18 | N5 | C19 | 122.22(14) |  | C13 | C12 | C11 | 113.53(11) |
| C23 | N6 | C24 | 115.1(5) |  | N4 | C13 | C12 | 111.19(11) |
| C23A | N6A | C24A | 115.9(5) |  | N4 | C13 | C14 | 109.40(12) |
| N1 | C4 | C3 | 124.34(19) |  | C14 | C13 | C12 | 110.70(11) |
| C4 | C3 | C2 | 118.15(18) |  | C13 | C14 | C9 | 112.92(12) |
| C3 | C2 | C1 | 119.66(16) |  | O2 | C18 | N4 | 123.16(13) |
| C2 | C1 | C5 | 116.40(17) |  | O2 | C18 | N5 | 122.38(13) |
| C2 | C1 | C6 | 122.87(14) |  | N4 | C18 | N5 | 114.46(13) |
| C5 | C1 | C6 | 120.72(16) |  | N5 | C19 | C20 | 122.4(2) |
| N1 | C5 | C1 | 125.73(19) |  | N5 | C19 | C20A | 105.3(2) |
| N2 | C6 | C1 | 114.10(13) |  | C21 | C20 | C19 | 125.3(5) |
| O1 | C7 | N2 | 121.44(14) |  | C21 | C20 | C24 | 117.2(5) |
| O1 | C7 | N3 | 123.48(14) |  | C24 | C20 | C19 | 117.3(5) |
| N3 | C7 | N2 | 115.08(14) |  | C21A | C20A | C19 | 125.0(4) |
| N3 | C8 | C9 | 114.34(11) |  | C24A | C20A | C19 | 117.4(4) |
| C10 | C9 | C8 | 106.85(11) |  | C24A | C20A | C21A | 117.3(5) |
| C14 | C9 | C8 | 109.10(12) |  | C20 | C21 | C22 | 119.5(4) |
| C14 | C9 | C10 | 109.27(11) |  | C20A | C21A | C22A | 119.5(4) |
| C14 | C9 | C15 | 110.72(12) |  | C23 | C22 | C21 | 118.5(4) |
| C15 | C9 | C8 | 108.59(12) |  | C23A | C22A | C21A | 118.2(4) |
| C15 | C9 | C10 | 112.19(12) |  | N6 | C23 | C22 | 124.0(6) |
| C11 | C10 | C9 | 117.86(11) |  | N6A | C23A | C22A | 124.0(6) |
| C12 | C11 | C10 | 108.92(11) |  | N6 | C24 | C20 | 125.7(5) |
| C16 | C11 | C10 | 113.07(12) |  | N6A | C24A | C20A | 125.2(5) |

| Table 6 Hydrogen Bonds for 23srv389. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| D | H | A | d(D-H)/Å | d(H-A)/Å | d(D-A)/Å | D-H-A/° |
| N3 | H3 | O21 | 0.888(17) | 2.003(17) | 2.8858(17) | 172.4(15) |
| N5 | H5 | O12 | 0.845(17) | 2.132(17) | 2.9465(17) | 161.7(14) |

11-X,-Y,1-Z; 21-X,-Y,2-Z

| Table 7 Torsion Angles for 23srv389. |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A | B | C | D | Angle/˚ |  | A | B | C | D | Angle/˚ |
| N1 | C4 | C3 | C2 | 0.8(3) |  | C11 | C12 | C13 | C14 | -57.46(16) |
| N3 | C8 | C9 | C10 | 178.50(12) |  | C12 | C13 | C14 | C9 | 57.62(15) |
| N3 | C8 | C9 | C14 | -63.48(16) |  | C13 | N4 | C18 | O2 | -5.8(2) |
| N3 | C8 | C9 | C15 | 57.29(16) |  | C13 | N4 | C18 | N5 | 173.91(12) |
| N4 | C13 | C14 | C9 | -179.51(11) |  | C14 | C9 | C10 | C11 | 48.64(17) |
| N5 | C19 | C20 | C21 | -128.4(2) |  | C15 | C9 | C10 | C11 | -74.55(16) |
| N5 | C19 | C20 | C24 | 45.8(3) |  | C15 | C9 | C14 | C13 | 72.28(15) |
| N5 | C19 | C20A | C21A | -73.1(5) |  | C16 | C11 | C12 | C13 | -73.58(15) |
| N5 | C19 | C20A | C24A | 113.6(4) |  | C17 | C11 | C12 | C13 | 168.60(12) |
| C4 | N1 | C5 | C1 | 0.9(3) |  | C18 | N4 | C13 | C12 | -101.35(15) |
| C4 | C3 | C2 | C1 | -0.2(2) |  | C18 | N4 | C13 | C14 | 136.07(13) |
| C3 | C2 | C1 | C5 | 0.1(2) |  | C18 | N5 | C19 | C20 | -87.4(3) |
| C3 | C2 | C1 | C6 | 179.31(15) |  | C18 | N5 | C19 | C20A | -90.7(3) |
| C2 | C1 | C5 | N1 | -0.5(3) |  | C19 | N5 | C18 | O2 | -8.1(2) |
| C2 | C1 | C6 | N2 | 40.8(2) |  | C19 | N5 | C18 | N4 | 172.15(12) |
| C5 | N1 | C4 | C3 | -1.1(3) |  | C19 | C20 | C21 | C22 | 174.3(3) |
| C5 | C1 | C6 | N2 | -140.01(15) |  | C19 | C20 | C24 | N6 | -174.7(3) |
| C6 | N2 | C7 | O1 | 3.9(2) |  | C19 | C20A | C21A | C22A | -173.7(3) |
| C6 | N2 | C7 | N3 | -175.84(14) |  | C19 | C20A | C24A | N6A | 174.8(4) |
| C6 | C1 | C5 | N1 | -179.70(17) |  | C20 | C21 | C22 | C23 | -0.1(3) |
| C7 | N2 | C6 | C1 | -90.83(18) |  | C20A | C21A | C22A | C23A | -0.4(5) |
| C7 | N3 | C8 | C9 | 96.89(16) |  | C21 | C20 | C24 | N6 | 0.1(3) |
| C8 | N3 | C7 | O1 | 12.4(2) |  | C21 | C22 | C23 | N6 | 0.1(4) |
| C8 | N3 | C7 | N2 | -167.93(12) |  | C21A | C20A | C24A | N6A | 0.9(7) |
| C8 | C9 | C10 | C11 | 166.55(12) |  | C21A | C22A | C23A | N6A | 0.8(7) |
| C8 | C9 | C14 | C13 | -168.27(11) |  | C23 | N6 | C24 | C20 | 0.0(3) |
| C9 | C10 | C11 | C12 | -48.03(17) |  | C23A | N6A | C24A | C20A | -0.5(7) |
| C9 | C10 | C11 | C16 | 74.87(16) |  | C24 | N6 | C23 | C22 | -0.1(3) |
| C9 | C10 | C11 | C17 | -166.60(12) |  | C24 | C20 | C21 | C22 | 0.0(2) |
| C10 | C9 | C14 | C13 | -51.78(15) |  | C24A | N6A | C23A | C22A | -0.4(8) |
| C10 | C11 | C12 | C13 | 51.02(15) |  | C24A | C20A | C21A | C22A | -0.4(6) |
| C11 | C12 | C13 | N4 | -179.28(12) |  |  |  |  |  |  |

| Table 8 Hydrogen Atom Coordinates (Å×104) and Isotropic Displacement Parameters (Å2×103) for 23srv389. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Atom | x | y | z | U(eq) |
| H2 | 5369(7) | -1606(7) | 6550(20) | 37(5) |
| H3 | 4501(7) | -1314(7) | 5860(19) | 42(5) |
| H4 | 4821(7) | 1007(7) | 8700(20) | 47(5) |
| H5 | 5536(7) | 1606(6) | 9082(19) | 35(5) |
| H1 | 7327.43 | 22.6 | 9313.72 | 73 |
| H2A | 6351.15 | 297.65 | 9087.72 | 59 |
| H3A | 5639.33 | -433.38 | 8680.98 | 49 |
| H5A | 6936.71 | -1628.09 | 8730.13 | 67 |
| H6A | 6006.96 | -1962.94 | 8061.24 | 53 |
| H6B | 5603.95 | -1720.46 | 9341.82 | 53 |
| H8A | 3763.5 | -820.28 | 7929.95 | 37 |
| H8B | 3542.54 | -1038.89 | 6384.92 | 37 |
| H10A | 3022.52 | -94.07 | 5858.85 | 36 |
| H10B | 3164.92 | -17.8 | 7530.35 | 36 |
| H12A | 3755.93 | 1477.83 | 7044.6 | 34 |
| H12B | 3673.24 | 1000.74 | 8294.82 | 34 |
| H13 | 4446.72 | 869.09 | 5873.39 | 33 |
| H14A | 4305.16 | 65.96 | 8232.16 | 34 |
| H14B | 4767.9 | -14.57 | 6947.96 | 34 |
| H15A | 4178.41 | 174.88 | 4378.43 | 51 |
| H15B | 3751.15 | -376.83 | 4150.47 | 51 |
| H15C | 4423.8 | -479.09 | 4593.48 | 51 |
| H16A | 3155.88 | 1380.2 | 4761.21 | 48 |
| H16B | 2999.21 | 727.68 | 4239.84 | 48 |
| H16C | 3671.7 | 919.78 | 4436.66 | 48 |
| H17A | 2635.71 | 831.44 | 8028.62 | 51 |
| H17B | 2340.76 | 764.63 | 6470.63 | 51 |
| H17C | 2622.14 | 1379.9 | 6947.51 | 51 |
| H19A | 6037.09 | 2443.39 | 8684.09 | 43 |
| H19B | 5845.71 | 2401.4 | 7041.22 | 43 |
| H19C | 6060.18 | 2456.08 | 8647.7 | 43 |
| H19D | 5891.82 | 2382.64 | 6971.46 | 43 |
| H21 | 7106.84 | 2492.61 | 8718.74 | 40 |
| H21A | 6728.93 | 1529.99 | 9687.03 | 41 |
| H22 | 8007.73 | 2051.03 | 8090.25 | 41 |
| H22A | 7613.24 | 1044.73 | 9115.93 | 48 |
| H23 | 8010 | 1276.1 | 6491.11 | 44 |
| H23A | 7917.11 | 1015.95 | 6744.37 | 56 |
| H24 | 6298.98 | 1358.06 | 6108.98 | 44 |
| H24A | 6553.1 | 1937.71 | 5519.44 | 47 |

| Table 9 Atomic Occupancy for 23srv389. |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Atom | Occupancy |  | Atom | Occupancy |  | Atom | Occupancy |
| N6 | 0.484(2) |  | N6A | 0.516(2) |  | H19A | 0.484(2) |
| H19B | 0.484(2) |  | H19C | 0.516(2) |  | H19D | 0.516(2) |
| C20 | 0.484(2) |  | C20A | 0.516(2) |  | C21 | 0.484(2) |
| H21 | 0.484(2) |  | C21A | 0.516(2) |  | H21A | 0.516(2) |
| C22 | 0.484(2) |  | H22 | 0.484(2) |  | C22A | 0.516(2) |
| H22A | 0.516(2) |  | C23 | 0.484(2) |  | H23 | 0.484(2) |
| C23A | 0.516(2) |  | H23A | 0.516(2) |  | C24 | 0.484(2) |
| H24 | 0.484(2) |  | C24A | 0.516(2) |  | H24A | 0.516(2) |

Refinement model description

Number of restraints - 18, number of constraints - unknown.

Details:

1. Fixed Uiso
 At 1.2 times of:
  All C(H) groups, All C(H,H) groups, All C(H,H,H,H) groups
 At 1.5 times of:
  All C(H,H,H) groups
2. Restrained distances
 C19-C20 ≈ C19-C20A
 with sigma of 0.02
 C20-C24 ≈ C20A-C24A
 with sigma of 0.02
 C20-C21 ≈ C20A-C21A
 with sigma of 0.02
 N6-C23 ≈ N6A-C23A
 with sigma of 0.02
 N6-C24 ≈ N6A-C24A
 with sigma of 0.02
 C23-C22 ≈ C23A-C22A
 with sigma of 0.02
 C21-C22 ≈ C21A-C22A
 with sigma of 0.02
 C19-C24 ≈ C19-C24A
 with sigma of 0.04
 C19-C21 ≈ C19-C21A
 with sigma of 0.04
 C20-N6 ≈ C20A-N6A
 with sigma of 0.04
 C20-C22 ≈ C20A-C22A
 with sigma of 0.04
 N6-C22 ≈ N6A-C22A
 with sigma of 0.04
 C23-C24 ≈ C23A-C24A
 with sigma of 0.04
 C23-C21 ≈ C23A-C21A
 with sigma of 0.04
 C24-C21 ≈ C24A-C21A
 with sigma of 0.04
3. Restrained planarity
 N6, C20, C21, C22, C23, C24
 with sigma of 0.01
4. Others
 Sof(N6A)=Sof(H19C)=Sof(H19D)=Sof(C20A)=Sof(C21A)=Sof(H21A)=Sof(C22A)=
 Sof(H22A)=Sof(C23A)=Sof(H23A)=Sof(C24A)=Sof(H24A)=1-FVAR(1)
 Sof(N6)=Sof(H19A)=Sof(H19B)=Sof(C20)=Sof(C21)=Sof(H21)=Sof(C22)=Sof(H22)=
 Sof(C23)=Sof(H23)=Sof(C24)=Sof(H24)=FVAR(1)
5.a Ternary CH refined with riding coordinates:
 C13(H13)
5.b Secondary CH2 refined with riding coordinates:
 C6(H6A,H6B), C8(H8A,H8B), C10(H10A,H10B), C12(H12A,H12B), C14(H14A,H14B),
 C19(H19A,H19B), C19(H19C,H19D)
5.c Aromatic/amide H refined with riding coordinates:
 C4(H1), C3(H2A), C2(H3A), C5(H5A), C21(H21), C21A(H21A), C22(H22), C22A(H22A),
  C23(H23), C23A(H23A), C24(H24), C24A(H24A)
5.d Idealised Me refined as rotating group:
 C15(H15A,H15B,H15C), C16(H16A,H16B,H16C), C17(H17A,H17B,H17C)

This report has been created with Olex2, compiled on 2023.08.24 svn.re1ec1418 for OlexSys. Please let us know if there are any errors or if you would like to have additional features.